1.	MANUFACTURING PROCESS

CIREBELLE waxes are uniquely derived from natural sources by means of the Fischer-Tropsch process.  Natural gas and air is converted to carbon monoxide and hydrogen gas.  The waxes are produced by way of catalytic reaction of the hydrogen and carbon monoxide at elevated temperature and pressure. Multiple processes such as distillation, purification and modification render these waxes of exceptional purity.  Continuous and thorough quality control is maintained throughout the manufacturing process to ensure consistent, high quality waxes for the cosmetics and toiletries market.

2.	CHEMICAL AND PHYSICAL PROPERTIES

CIREBELLE waxes are long-chain, unbranched hydrocarbons with the following chemical structure: CH3-(CH2)n-CH3.  The molecular weights of the individual waxes range from 300 to 1000 Daltons.  The melting point increases with increasing molecular weight and cover the range from 40 ºC to 100ºC.   The waxes are pure white and not translucent, having a fine crystalline structure.  The inert nature of Fischer-Tropsch waxes ensures the absence of side reactions with other ingredients.

Due to the nature of the manufacturing process, the purity of CIREBELLE waxes is high and they are free from sulphur and aromatic compounds.  A further result of this is that the waxes are classified as non-irritant and practically odourless.

The high melting point and hardness of certain CIREBELLE waxes impart an increase in the melting point and hardness of wax and oil blends such as sticks.

3.	PRODUCT RANGE

CIREBELLE 109L is a high melting wax (90ºC) specifically tailored to comply with the Colipa recommendations for lip products. This tasteless and odourless wax provides hardness and strength to stick formulations without imparting a waxy feel or taste on application.

CIREBELLE 108 is another high melting wax (80ºC) offering exceptional benefits to skin- and lip-care products.  In stick formulations, it replaces waxes like Carnauba and Candelilla, imparting temperature stability, strength and hardness. Its film forming property makes it an ideal ingredient for creams and lotions rendering a non waxy, velvety feel. CIREBELLE 108 is also used- with great success in w/o emulsions, e.g. body butters.

CIREBELLE 303 is a highly economical wax used in a variety of applications ranging from skin- and lip-care (lip balms) to hair-care (hair relaxers).  In o/w emulsions it is used effectively to improve the gloss and whiteness of the emulsion, in addition to providing an elegant skin feel.

CIREBELLE 305 was specifically developed as an ingredient for hair relaxers where it has been found to have excellent performance and assists in ease of manufacture (no homogenisation is required).  This wax is also an ideal emollient for skin- and body-care.  In sun-care it imparts water resistance.

CIREBELLE 505 possesses a very low melting point - just above body temperature.  In creams and lotions it offers a unique skin feel, excellent spreading, and good film forming properties.

CIREBELLE waxes can be easily emulsified and form excellent cosmetic creams and lotions with relatively low percentages of emulsifiers.

4.	APPLICATION MATRIX

| WAX | MELTING POINT (ºC) | EMULSION | STICK | POMADE |
| --- | --- | --- | --- | --- |
| CIREBELLE 109L | 91 - 96 | ● | ●●● |  |
| CIREBELLE 108 | 79 – 84 | ● | ●●● | ●● |
| CIREBELLE 303 | 61 – 67 | ●●● | ●● | ●● |
| CIREBELLE 305 | 55 – 62 | ●●● | ●● | ●● |
| CIREBELLE 505 | 38 - 42 | ●●● | ●● | ●●● |

Best suited	●●●

Well applicable	●●

Applicable	●

5.	ANTI-AGEING PROPERTIES

Three waxes, selected to cover the spread of our range of waxes, were evaluated against an industry standard in a scientific study.  In each case, 5% of Fischer Tropsch wax replaced the same weight of caprylic triglyceride (CTG) in a moisturising cream containing 10% CTG, i.e. the control had 10% CTG, whereas the test samples contained 5% each of wax and CTG.  After 28 days of twice a day application to the inner sides of the forearms of volunteers, the following average improvements were measured as compared to untreated skin and the control respectively:

| MEASUREMENT | %improvement (untreated skin) | %improvement (control) |
| --- | --- | --- |
| Skin firmness (elasticity) | 22 | 14 |
| Skin smoothness (roughness reduction) | 30 | 9 |
| Skin hydration | 26 | 14 |

Skin firmness, skin smoothness and skin hydration were measured by means of Cutometer, Phase-shifting Rapid In vivo Measurement of the Skin (PRIMOS) and Corneometer respectively.

6.	SAFETY AND TOXICITY

A summary of safety and toxicity test results follows here.  More detail of the actual test can be obtained upon request.

Human Repeat Insult Patch Test

CIREBELLE 505	Hypo allergenic (100%) and Non-irritant (100%)

CIREBELLE 305	Hypo allergenic (100%) and Non-irritant (100%)

CIREBELLE 109L 	Hypo allergenic (100%) and Non-irritant (100%)

In Vito evaluation of Acute Ocular Tolerance

CIREBELLE 505	Not cytotoxic / non-irritant to cells of the reconstituted cornea

CIREBELLE 305	Not cytotoxic / non-irritant to cells of the reconstituted cornea

CIREBELLE 109L	Not cytotoxic / non-irritant to cells of the reconstituted cornea

Skin Patch test

CIREBELLE 303	Non-irritant

CIREBELLE 108	Non-irritant

Moisturising cream containing 15% CIREBELLE 303	                    Non-irritant

Waxes identical in composition to these Fischer-Tropsch waxes have been tested for mutagenicity (Ames Salmonella / Microsome Plate test) and were found to be non mutagenic.

7.	GUIDELINE FORMULATIONS

| ULTRA RICH MOISTURISING CREAM |
| --- |
| FORM. REF. NO.: SC 005-1003 A |
|  | TRADE NAME | INCI NAME | % |
| A | Water (Purified) | Water | 68.30 |
|  | Carbopol Ultrez 10 Polymer | Carbomer | 0.20 |
| B | Glycerine | Glycerin | 4.00 |
|  | Allantoin | Allantoin | 0.20 |
|  | Sequestrene Na2 | Disodium EDTA | 0.10 |
| C | BHT | BHT | 0.10 |
|  | CIREBELLE 505 | Synthetic Wax | 5.00 |
|  | Silicone Oil DC 556 | Phenyl Trimethicone | 2.00 |
|  | Lexol GT865/ Neobee M5 | Caprylic/Capric Triglyceride | 3.00 |
|  | Arlacel 165 | Glyceryl Stearate (and) PEG-100 Stearate | 4.00 |
|  | Sweet Almond Oil | Prunus Amygdalus Dulcis (Sweet Almond) Oil | 2.00 |
|  | Jojoba Oil | Simmondsia Chinensis (Jojoba) Seed Oil | 2.00 |
|  | Polawax GP200 | Cetearyl Alcohol (and) PEG-20 Stearate | 2.00 |
|  | Cetyl Alcohol | Cetyl Alcohol | 2.00 |
|  | Dragosantol | Bisabolol | 0.50 |
|  | Vitamin E Acetate | Tocopheryl Acetate | 0.50 |
| D | Triethanolamine 99% | Triethanolamine | 0.30 |
|  | Germaben II | Propylene Glycol (and) Diazolidinyl Urea (and) Methylparaben (and) Propylparaben | 0.80 |
| E | Pentavitin | Saccharide Isomerate | 3.00 |
|  |  |  | 100.00 |
|  | MANUFACTURING METHOD |
| A | Heat water up to 75-80ºC. Disperse Carbopol Ultrez 10 polymer using a high shear mixer. |
| B | Add ingredients B to water phase. Keep the water phase at 75-80ºC. |  |
| C | In another kettle, charge ingredients from part C. Heat up to 75-80ºC and mix until all ingredients are melted. |
|  | Add oil phase (C) at 75-80ºC to water phase (A+B) at 75-80ºC and homogenise for 15-20 min. |
| D | Add Triethanolamine and mix for another 5 min. Replace high shear mixer with counter mixer. |
|  | While mixing, slowly cool the bulk to 35-40ºC. |
| E | Add Pentavitin and Germaben II. Mix slowly. |

| SUNSCREEN STICK SPF 30 - water resistant |
| --- |
| FORM. REF. NO.: SS 01-0203 |
|  | TRADE NAME | INCI NAME | % |
| A | Parsol MCX | Ethylhexyl Methoxycinnamate | 3.00 |
|  | Parsol 1789 | Butyl Methoxydibenzoylmethane | 1.00 |
|  | Parsol 5000 | 4 - Methylbenzylidene Camphor | 4.00 |
|  | Uvinul M 40 | Benzophenone-3 | 2.00 |
|  | Finsolv TN | C12-15 Alkyl Benzoate | 5.00 |
|  | Miglyol 829 | Caprylic/Capric/Succinic Triglyceride | 5.00 |
|  | Propyl Paraben | Propylparaben | 0.20 |
|  | Acetulan | Cetyl Acetate (and) Acetylated Lanolin Alcohol | 10.00 |
|  | Antaron V-216 | VP / Hexadecene Copolymer | 3.00 |
|  | Cetiol OE | Dicaprylyl Ether | 9.00 |
|  | Lexol GT865/ Neobee M5 | Caprylic/Capric Triglyceride | 14.30 |
|  | CIREBELLE 303 | Synthetic Wax | 10.00 |
|  | CIREBELLE 108 | Synthetic Wax | 12.00 |
| B | Zinc Oxide BP | Zinc Oxide | 7.00 |
|  | Talc (Micronized) | Talc | 4.00 |
| C | Silicone DC 245 | Cyclomethicone | 10.00 |
|  | Vitamin E Acetate | Tocopheryl Acetate | 0.50 |
|  |  |  | 100.00 |
|  | MANUFACTURING METHOD |
| A | Heat ingredients (A) up to 85ºC and mix until all ingredients have melted (clear). |
| B | Disperse powders using a high shear mixer until mass is homogeneous. Cool the batch to 80ºC. |
| C | Add Silicone DC 245 and Vitamin E Acetate and mix well. Pour at 75 - 80ºC while mixing slowly. |

| HAND AND BODY CREAM FORM. REF. NO : BC 03-0802 |
| --- |
|  | TRADE NAME | INCI NAME | % |
| A | Water Purified | Water | 67.80 |
|  | Carbopol Ultrez 10 Polymer | Carbomer | 0.20 |
| B | Propylene Glycol | Propylene Glycol | 4.00 |
|  | Methyl Paraben | Methylparaben | 0.20 |
|  | Sequestrene Na2 | Disodium EDTA | 0.10 |
| C | Stearic Acid PHO 5 | Stearic Acid | 2.50 |
|  | Tween 60 | Polysorbate 60 | 0.50 |
|  | Mineral Oil | Mineral Oil | 5.00 |
|  | Silicone DC 200/1000 | Dimethicone | 1.00 |
|  | Glyceryl Monostearate S/E | Glyceryl Stearate | 2.00 |
|  | Propyl Paraben | Propylparaben | 0.20 |
|  | CIREBELLE 303 | Synthetic Wax | 5.00 |
|  | CIREBELLE 505 | Synthetic Wax | 5.00 |
|  | Lexol GT 865 | Caprylic/ Capric Triglyceride | 4.00 |
| D | Triethanolamine 99% | Triethanolamine | 1.20 |
| E | Water Purified | Water | 1.00 |
|  | Germall 115 | Imidazolidinyl Urea | 0.30 |
|  |  |  | 100.00 |
|  |  | MANUFACTURING METHOD |
| A | Heat water up to 75-80ºC. Disperse Carbopol Ultrez 10 polymer using a high shear mixer. |  |
| B | Add all ingredients to water and mix. Keep the water phase at 75-80ºC. |  |
| C | Charge all ingredients into second kettle. Heat up to 75-80ºC and mix until all ingredients have melted. |
|  | Add oil phase (C) at 75-80ºC to water (A +B) phase at 75-80ºC and mix with a high shear mixer for 10-15 min. |  |
| D | Add TEA concentrate to the bulk at 75ºC minimum and mix for another 5-10min. Replace high shear |  |
|  | mixer with counter mixer. Cool the bulk to 35-40ºC. |  |
| E | Pre-dissolve Germall 115 in second part of water (clear solution) and add to the bulk. Mix well. |  |

| ANTIPERSPIRANT ROLL-ON FORM. REF. NO.: AB 02-1003 D |
| --- |
|  | TRADE NAME | INCI NAME | % |
| A | Water Purified | Water | 59.8 |
|  | Propylene Glycol | Propylene Glycol | 6.00 |
| B | Aluminium Chlorhydroxide | Aluminum Chlorhydrate | 20.0 |
| C | GMS Acid Stable | Glyceryl Stearate (and) PEG-100 Stearate | 2.00 |
|  | Polawax GP200 | Cetearyl Alcohol (and) PEG-20 Stearate | 5.00 |
|  | CIREBELLE 303 | Synthetic wax | 4.00 |
|  | Irgasan DP 300 | Triclosan | 0.20 |
| D | Tween 20 | Polysorbate 20 | 2.00 |
|  | Perfume | Fragrance | 1.00 |
|  |  |  | 100.00 |
|  |  | MANUFACTURING METHOD |
| A | Heat water up to 75-80ºC. Insert high shear mixer and then add Propylene Glycol. |  |
| B | Add Aluminium Chlorhydroxide to water phase using a high shear mixer. Keep the water phase at 75-80 ºC. |  |
| C | In another kettle, charge ingredients from part C. Heat up to 75-80ºC and mix until melted. Add oil phase (C) |
|  | at 75-80ºC to water phase (A+B) at 75-80ºC and homogenise for 15-20 min. Replace high shear mixer with |  |
|  | propeller mixer. While mixing slowly cool the bulk to 35-40ºC. |  |
| D | Pre-mix Tween 20 and Perfume and add to the bulk. Mix slowly but well. |  |

| MOISTURISING BODY SPRAY FORM. REF. NO.: BC 022-1103 D |
| --- |
|  | TRADE NAME | INCI NAME | % |
| A | Water Purified | Water | 69.20 |
|  | Veegum HV | Magnesium Aluminum Silicate | 0.20 |
| B | Propylene Glycol | Propylene Glycol | 4.00 |
|  | Allantoin | Allantoin | 0.20 |
|  | TEA Concentrate 99% | Triethanolamine | 1.50 |
|  | Sequestrene Na2 | Disodium EDTA | 0.10 |
| C | Stearic Acid PHO 5 | Stearic Acid | 1.50 |
|  | Tween 60 | Polysorbate 60 | 3.00 |
|  | Silicone DC 556 | Phenyl Trimethicone | 3.00 |
|  | Glyceryl Monostearate S/E | Glyceryl Stearate | 1.00 |
|  | Span 60 | Sorbitan Stearate | 0.50 |
|  | Lexol GT 865 | Caprylic/ Capric Triglyceride | 4.00 |
|  | CIREBELLE 505 | Synthetic Wax | 4.00 |
| D | Alcohol Absolute Denatured | Alcohol Denatured | 5.00 |
|  | Hydroviton 2/059353 | Water (and) Glycerin (and) Sodium Lactate (and) | 2.00 |
|  |  | TEA-Lactate (and) Serine (and) Lactic Acid (and) Urea |  |
|  |  | (and) Sorbitol (and) Sodium Chloride (and) Lauryl |  |
|  |  | Diethylenediaminoglycine (and) Lauryl |  |
|  |  | Aminopropylglycine (and) Allantoin |  |
|  | Germaben II | Propylene Glycol (and) Diazolidinyl Urea (and) | 0.80 |
|  |  | Methylparaben (and) Propylparaben |  |
|  |  |  | 100.00 |
|  |  | MANUFACTURING METHOD |
| A | Heat water up to 75-80ºC. Hydrate Veegum HV using a high shear mixer. |  |
| B | Add all ingredients to water and mix. Keep the water phase at 75-80ºC. |  |
| C | Charge all ingredients into second kettle. Heat up to 75-80ºC and mix until all ingredients have melted. |
|  | Add oil phase (C) at 75-80ºC to water (A +B) phase at 75-80ºC and mix with a high shear mixer for 10-15 min. |  |
| D | Cool the bulk to 40-45°C using a propeller mixer. Add ingredients from part D. |  |

| MOISTURISING LIPSTICK REF. No.: CL 15 - 0403 |
| --- |
|  | TRADE NAME | INCI NAME | % |
| A | Lexol GT 865 | Caprylic/Capric Triglyceride | 7.50 |
|  | Propyl Paraben | Propylparaben | 0.20 |
|  | BHT | BHT | 0.10 |
| B | Castor Oil BP | Ricinus Communis (Castor) Seed Oil | 36.70 |
|  | Crodalan LA | Cetyl Acetate (and) Acetylated Lanolin Alcohol | 9.00 |
|  | Beeswax | Beeswax | 1.00 |
|  | Ozokerite | Ozokerite | 0.50 |
|  | CIREBELLE 108 | Synthetic Wax | 4.00 |
|  | Carnauba Wax | Copernicia Cerifera (Carnauba) Wax | 7.00 |
|  | Abil Wax 9801 | Cetyl Dimethicone | 5.00 |
|  | Crodamol PC | Propylene Glycol Dicaprylate / Dicaprate | 4.00 |
|  | Fluilan | Lanolin Oil | 5.00 |
| C | Pro Lip White | Ricinus Communis (Castor) Seed Oil & Titanium Dioxide | 4.00 |
|  |  | (and) BHT (and) Lecithin |  |
|  | Pro Lip Mustard | Ricinus Communis (Castor) Seed Oil (and) Yellow Iron | 1.00 |
|  |  | Oxide (and) BHT |  |
|  | Pro Lip Red 21 | Ricinus Communis (Castor) Seed Oil (and) D&C Red | 2.00 |
|  |  | No.21 Aluminium Lake (and) BHT |  |
|  | Pro Lip Russet | Ricinus Communis (Castor) Seed Oil (and) Red Iron Oxide | 2.00 |
|  | Pro Lip Black | Ricinus Communis (Castor) Seed Oil (and) Black Iron | 1.00 |
|  |  | Oxide (and) BHT |  |
|  | Cloisonne Rouge | Mica (and) Titanium Dioxide (and) Iron Oxides | 6.00 |
|  | Cloisonne Bronze | Mica (and) Titanium Dioxide (and) Iron Oxides | 2.00 |
|  | Cloisonne Gold | Mica (and) Titanium Dioxide (and) Iron Oxides | 2.00 |
|  |  |  | 100.00 |
|  |  | MANUFACTURING METHOD |
| A | Heat up to 75ºC and mix until powders are solubilised (clear). |  |
| B | Add ingredients from part B and heat up to 85 - 88ºC until all waxes have melted. |  |
| C | Add pigments and pearl. Mix well and pour into slightly warmed lipstick mould at 78 - 83ºC. |

| FACE CREAM SPF 15-18 (with organic sunscreens) FORM. REF. NO.: SC 059-0104 A |
| --- |
|  | TRADE NAME | INCI NAME | % |
| A | Water Purified | Water | 58.60 |
|  | Carbopol Ultrez 10 Polymer | Carbomer | 0.30 |
| B | Glycerine | Glycerin | 3.00 |
|  | Allantoin | Allantoin | 0.20 |
|  | Sequestrene Na2 | Disodium EDTA | 0.10 |
| C | Parsol MCX | Ethylhexyl Methoxycinnamate | 3.00 |
|  | Parsol 1789 | Butyl Methoxydibenzoylmethane | 2.00 |
|  | Parsol 5000 | 4 - Methylbenzylidene Camphor | 2.00 |
|  | Finsolv TN | C12-15 Alkyl Benzoate | 3.00 |
| D | CIREBELLE 303 | Synthetic Wax | 6.00 |
|  | Silicone DC 245 | Cyclopentasiloxane | 3.00 |
|  | Lexol GT865/ Neobee M5 | Caprylic/Capric Triglyceride | 2.00 |
|  | Span 60 | Sorbitan Stearate | 2.50 |
|  | Tween 60 | Polysorbate 60 | 1.50 |
|  | Cetyl Alcohol | Cetyl Alcohol | 2.00 |
| E | Triethanolamine 99% | Triethanolamine | 0.40 |
| F | Sepigel 305 | Polyacrylamide (and) C13-14 Isoparaffin (and) Laureth-7 | 1.00 |
| G | Eusolex 232 Powder | Phenylbenzimidazole Sulfonic Acid | 2.90 |
|  | Triethanolamine 99% | Triethanolamine | 1.70 |
|  | Water Purified | Water | 4.00 |
| H | Germaben II | Propylene Glycol (and) Diazolidinyl Urea (and) | 0.80 |
|  |  | Methylparaben (and) Propylparaben |  |
|  |  |  | 100.00 |
|  |  | MANUFACTURING METHOD |
| A | Heat the water up to 75-80ºC. Disperse Carbopol Ultrez 10 polymer using a high shear mixer. |  |
| B | Add ingredient B to water phase. Keep the water phase at 75-80ºC. |  |
| C | In another kettle, charge ingredients from part C. Heat up to 75-80ºC and mix (clear solution). |
| D | Add ingredients to oil phase and mix until all ingredients have melted. Add oil phase (C + D) at 75-80°C to |  |
|  | water phase (A+B) at 75-80ºC and homogenise for 15-20 min. |  |
| E | Add Triethanolamine and mix. |  |
| F | Add Sepigel 305 and mix. Replace high shear mixer with counter rotating mixer. While mixing slowly, cool |  |
|  | the bulk to 35-40ºC. |  |
| G | Solubilise Eusolex 232 while heating (clear solution). Add solution D while mixing slowly. |  |
| H | Add Germaben II and mix slowly. |  |

| COVER STICK |
| --- |
| FORM. REF. NO.: CC 01-1002 |
|  | TRADE NAME | INCI NAME | % |
| A | Lexol GT865/ Neobee M5 | Caprylic/Capric Triglyceride | 12.00 |
|  | Lonzest 143-S | Myristyl Propionate | 5.00 |
|  | Silicone DC 245 | Cyclopentasiloxane | 10.00 |
|  | Crodalan LA | Cetyl Acetate ( and ) Acetylated Lanolin Alcohol | 8.00 |
|  | Castor Oil BP | Ricinus Communis (Castor) Seed Oil | 24.70 |
|  | Abil Wax 9801 | Cetyl Dimethicone | 5.00 |
|  | Beeswax (Bleached) | Beeswax | 3.00 |
|  | Candelilla Wax Flakes | Euphorbia Cerifera (Candelilla) Wax | 4.00 |
|  | CIREBELLE 108 | Synthetic Wax | 5.00 |
|  | Ozokerite Wax | Ozokerite | 3.00 |
|  | BHT | BHT | 0.10 |
|  | Propyl Paraben | Propylparaben | 0.20 |
| B | Titanium Dioxide | Titanium Dioxide | 15.20 |
|  | Brown C33-115 | Iron Oxides | 2.07 |
|  | Yellow C33-8073 | Iron Oxides | 2.33 |
|  | Black 318M | Iron Oxides | 0.40 |
|  |  |  | 100.00 |
|  | MANUFACTURING METHOD |
| A | Heat up to 85-88ºC. Mix until all ingredients have melted. |
| B | Wet the powders into phase A. Mix well with a high shear mixer at 85ºC. Cool to 75-80ºC and pour into |
|  | slightly warmed mould. |  |  |

| MOISTURISING BODY MILK |
| --- |
| FORM. REF. NO.: BM 02-0203 |
|  | TRADE NAME | INCI NAME | % |
| A | Water Purified | Water | 77.15 |
|  | Veegum HV | Magnesium Aluminum Silicate | 0.30 |
|  | Carbopol Ultrez 10 Polymer | Carbomer | 0.10 |
| B | Glycerine | Glycerin | 3.00 |
|  | Methyl Paraben | Methylparaben | 0.15 |
|  | TEA Concentrate 99% | Triethanolamine | 1.20 |
|  | Sequestrene Na2 | Disodium EDTA | 0.10 |
| C | Stearic Acid PHO 5 | Stearic Acid | 2.50 |
|  | Tween 60 | Polysorbate 60 | 1.00 |
|  | Silicone DC 200/1000 | Dimethicone | 2.00 |
|  | Propyl Paraben | Propylparaben | 0.20 |
|  | Lexol GT 865 | Caprylic/ Capric Triglyceride | 4.00 |
|  | CIREBELLE 505 | Synthetic Wax | 7.00 |
| D | Water Purified | Water | 1.00 |
|  | Germall 115 | Imidazolidinyl Urea | 0.30 |
|  |  |  | 100.00 |
|  | MANUFACTURING METHOD |
| A | Heat water up to 75-80ºC. Disperse Carbopol Ultrez 10 polymer using a high shear mixer. |  |
| B | Add all ingredients to water and mix. Keep the water phase at 75-80ºC. |  |
| C | Charge all ingredients into second kettle. Heat up to 75-80ºC and mix until all ingredients have melted. |
|  | Add oil phase (C) at 75-80ºC to water (A +B) phase at 75-80ºC and mix with a high shear mixer for 10-15 min. |
| D | Pre-dissolve Germall 115 in second part of water (clear solution) and add to the bulk. Mix well. |

| HAND & BODY LOTION |
| --- |
| FORM. REF. NO.: BL 34-0603 |  |
|  | TRADE NAME | INCI NAME | % |
| A | Water Purified | Water | 72.50 |
|  | Carbopol Ultrez 10 Polymer | Carbomer | 0.10 |
| B | Propylene Glycol | Propylene Glycol | 4.00 |
|  | Methyl Paraben | Methylparaben | 0.20 |
|  | Sequestrene Na2 | Disodium EDTA | 0.10 |
| C | Stearic Acid PHO 5 | Stearic Acid | 2.50 |
|  | Tween 60 | Polysorbate 60 | 1.00 |
|  | Mineral Oil | Mineral Oil | 5.00 |
|  | Silicone DC 200/1000 | Dimethicone | 1.00 |
|  | Glyceryl Monostearate S/E | Glyceryl Stearate | 2.00 |
|  | Propyl Paraben | Propylparaben | 0.20 |
|  | Petroleum Jelly | Petrolatum | 2.00 |
|  | Lexol GT 865 | Caprylic/ Capric Triglyceride | 3.00 |
|  | CIREBELLE 305 | Synthetic Wax | 4.00 |
| D | Triethanolamine 99% | Triethanolamine | 1.10 |
| E | Water Purified | Water | 1.00 |
|  | Germall 115 | Imidazolidinyl Urea | 0.30 |
|  |  |  | 100.00 |
|  | MANUFACTURING METHOD |
| A | Heat water up to 75-80ºC. Disperse Carbopol Ultrez 10 polymer using a high shear mixer. |  |
| B | Add all ingredients to water and mix. Keep the water phase at 75-80ºC. |  |
| C | Charge all ingredients into second kettle. Heat up to 75-80ºC and mix until all ingredients have melted. Add |
|  | oil phase (C) at 75-80ºC to water (A+B) phase at 75-80ºC and mix with a high shear mixer for up to 15min. |
| D | Add TEA concentrate to the bulk at 75ºC minimum and mix for another 5-10 min. Replace high shear |  |
|  | mixer with counter rotating mixer. Cool the bulk to 35-40ºC. |  |
| E | Pre-dissolve Germall 115 in second part of water (clear solution) and add to the bulk. Mix well. |

| AQUEOUS CREAM |
| --- |
| FORM. REF. NO.: BC 032-0803 |
|  | TRADE NAME | INCI NAME | % |
| A | Water Purified | Water | 61.70 |
|  | Triethanolamine 99% | Triethanolamine | 2.20 |
|  | SLS Needles | Sodium Lauryl Sulphate | 0.50 |
|  | Methyl Paraben | Methylparaben | 0.15 |
| B | Mineral Oil | Mineral Oil | 4.00 |
|  | Petroleum Jelly | Petrolatum | 12.00 |
|  | Stearic Acid Triple Pressed | Stearic Acid | 6.00 |
|  | CIREBELLE 305 | Synthetic wax | 8.00 |
|  | Cetyl Alcohol | Cetyl Alcohol | 4.00 |
|  | Propyl Paraben | Propylparaben | 0.15 |
| C | Water Purified | Water | 1.00 |
|  | Germall 115 | Imidazolidinyl Urea | 0.30 |
|  |  |  | 100.00 |
| MANUFACTURING METHOD |
| A | Heat the water phase A up to 80-85ºC. |  |  |
| B | Charge all ingredients into second kettle. Heat up to 80-85ºC and mix until all ingredients have melted. Add |
|  | oil phase (B) at 80-85ºC to water (A) phase at 80-85ºC and mix with a high shear mixer for 10-15 min. |  |
|  | Replace high shear mixer with counter mixer. Cool the bulk to 35-40ºC. |
| C | Pre-dissolve Germall 115 in second part of water (clear solution) and add to the bulk. Mix well. |  |

| ANTIPERSPIRANT STICK |  |
| --- | --- |
| FORM. REF. NO.: MP 061-0104 A |  |
|  | TRADE NAME | INCI NAME | % |
| A | Cetiol OE | Dicaprylyl Ether | 10.00 |
|  | Estol 3609 | Triethylhexanoin | 10.00 |
|  | Cutina HR | Hydrogenated Castor Oil | 4.00 |
|  | CIREBELLE 305 | Synthetic Wax | 15.70 |
|  | CIREBELLE 108 | Synthetic Wax | 3.30 |
| B | Starch (Corn Starch) | Zea Mays (Corn) Starch | 6.00 |
|  | Aluminium Chlorhydroxide | Aluminium Chlorhydrate | 16.00 |
|  | Bentone Gel VS-5PCV | Cyclopentasiloxane (and) Disteardimonium | 8.00 |
|  |  | Hectorite (and) Propylene Carbonate |  |
| C | Silicone DC 245 | Cyclopentasiloxane | 25.50 |
|  | Perfume | Fragrance | 1.50 |
|  |  |  | 100.00 |
|  | MANUFACTURING METHOD |
| A | Heat up to 85 - 90ºC and mix until all solids have melted. |  |  |
| B | Disperse powders and Bentone Gel one by one using a high shear mixer (Silverson). Mix until mass is |
|  | homogeneous. |  |
| C | Cool the bulk to 80 - 85ºC and add Silicone DC 245 and perfume. Mix well and pour at 75 - 80ºC (pouring |  |
|  | temperature will depend on type of packaging used). |  |

Technical Bulletin BEA 2005/002- Rev 2

Copyright April 2005

Although this information is presented in good faith and is believed to be, to the best of our knowledge, true and accurate, it has been compiled for information purposes only and without any warranty whatsoever. Due to the special nature of the products and their applications, we do not accept any responsibility or liability whatsoever that may result from the use of this information. If in doubt, please contact your local Sasol Wax office or distributor. The information contained herein is not to be construed as a license to operate under, or a recommendation to infringe upon, existing patents, nor should it be confused with any Governmental or insurance requirements or with any national or international safety codes.

# Text boxes

IMPROVED TEXTILE

PROCESSING

WITH

SASOLWAX AP5

CIREBELLE

WAXES

Sasolwax in COSMETICS